**Q25 Slab/ brick/ sett/ cobble pavings**

**310 NATURAL STONE SLABS**

* **Stone paving slabs to BS EN 1341:** For compliance to the Construction Products Regulations, a current CE Certificate and Declaration of Performance data sheet is available from Albion Stone which include declared values for each test listed below, based on at least 10 years of testing, and authorised by a company director.
  + Flexural Strength BSEN 13161
  + Slip Resistance BSEN 14231
  + Tactility (surface treatment)
  + Frost Resistance BSEN 12371
  + Thermal Shock Resistance BSEN 14066
  + Abrasion Resistance BSEN 141157
* **Face dimensions, length (l) x width (b):** NBS0091\_1BS.gif
* **Thickness (d):** Calculated using results from the CE Certificate for the Flexural strength – BSEN 13161 as per the method set out in Annex A, BSEN 1341.
* **Petrographic name to BS EN 12407:** Jurassic Limestone, Portland Whitbed from Jordans Mine
* **Denomination to BS EN 12440:** Portland Fancy Beach Whitbed
  + - Colour: Off white / creamy buff.
    - Origin: Portland, Dorset, UK
* **Finish:** The indicative sample reference number [insert] shows the surface finish, but not the full extent of the visual range. Range Panels located at Albion Stone’s mine in Portland show the range of geological features present in each bed of stone and will be the control samples for the project.
* **Supplier**: Albion Stone plc, Easton Street, Portland Dorset DT5 1BW. 01737 771772
* **Quality**: A Factory Production Control system will ensure the stone are free from vents, cracks, fissures, discolouration, or other defects deleterious to strength and durability. Tolerances as stated in BSEN 1341.
  + Quality Management: compliance with ISO 9001
* **Environmental impact.** 
  + Environmental Management: compliance with ISO 14001
  + Responsible Sourcing of the stone: compliance with BES 6001 - ‘Excellent certification’
  + Environmental Product Declaration (EPD) A1-A3 Global Warming Potential (GWP) 44.7kgCO2/Tonne
* *Note – all further sections to the specification should be in accordance with best practice as set out in the standard NBS clauses.*